## Slide 1
Bachelor Thesis 2
Mechanistic Study of CO2 methanation over Ru/TiO2
Under the supervision of
Dr. Koustuv Ray
Department of Chemical Engineering
Indian institute of Technology, Kharagpur
Arghadeep Biswas
21CH30049

## Slide 2
Hydrogenation of CO₂ to CH₄ (Sabatier reaction) is a promising method for CO₂ utilization.
Reaction is viable under mild conditions and produces CH₄ suitable for direct use or storage.
CH₄ can be transported using existing natural gas infrastructure.
CO₂ Methanation – A Key Utilization Route
Fig. 1: CO2 hydrogenation to produce CH4 via different catalysis methods (Li Li et. al.) [1]
Fig. 2 : Ruthenium on Titanium Dioxide support (Y. Zhang, et al.) [2]
Hydro
Catalytic Focus: Ru/TiO2
.
Ru/TiO₂ stands out for high CH₄ selectivity and activity under low temperatures.
TiO2 supports (anatase, rutile, Degussa P25) enhance activity via electronic interactions.
Reverse Water-Gas Shift (RWGS) reaction provides CO as an intermediate for methanation.
CO2 Methanation and Adsorption on Ru/TiO2
Notes: NASA and JAXA are also working on life support systems for closed-space environments where CO₂ methanation is necessary to maintain human operations [7]. In addition to methane, CO₂ hydrogenation can also yield useful chemicals such as methanol (CH₃OH), formaldehyde (HCHO), ethanol (C₂H₅OH), dimethyl ether (CH₃OCH₃), and higher hydrocarbons and oxygenates, providing fossil fuel alternatives

## Slide 3
CO₂ Methanation Performance Study CO₂ methanation over Ru/TiO₂ by varying temperature (150–400°C) and time (at 300°C) to determine optimal reaction conditions.
CO₂ Adsorption Behavior Analyze CO₂ adsorption on Ru/TiO₂ across temperatures (150–400°C) and at 200°C over time to understand surface intermediates and their stability.
In-situ DRIFTS Analysis Use in-situ DRIFTS to identify surface species formed during methanation and adsorption processes.
Reaction Pathway Correlation Correlate catalytic activity with surface coverage to propose potential reaction mechanisms.
Objective

## Slide 4
DRIFTS | Diffuse Reflectance Infrared Fourier Transform Spectroscopy
Where is Drifts used? How does it work?
Sample Properties:
Rough surfaces
Powders
Application examples:
Development of catalysts
Study temperature effects
Monitoring of reaction kinetics
Characterization of soil samples
Fig 3.
a Scheme of the diffuse reflectance accessory
b Course of the infrared radiation through an heterogeneous absorbing material [3]
The Harrick Praying Mantis
IR bean coming from the spectrometer is focused and directed at the sample
The sample diffusely scatters the incoming IR beam
The mirrors collect the scattered light and directed back to the spectrometer’s detector
Schematic drawing of Praying Mantis DRIFTS Cell

## Slide 5
Literature Review
Catalyst Screening for CO2 Methanation
Key Active Phases and Supports
Metals Studied: Ni, Co, Fe, Ru, Rh
Supports Used: SiO₂, Al₂O₃, CeO₂, TiO₂, ZrO₂, and mixed oxides
Advantages
High Activity and CH4 selectivity
Effective at low temperatures
Enhanced with optimized support choice
Catalyst | T (◦ C) | X CO2 (%) | S CH4 (%) | Ref.
2% wt. Ru/ TiO2 | 250oC | 20 | 100 | (Panagiotopoulou ,2017) [4]
3% wt. Ru/ Al2O3 | 300oC | 96 | 96 | (Garbarino et al., 2015) [5]
4% wt. Ru/ Al2O3 | 375oC | 85 | 100 | (Quindimil et al., 2015) [6]
1% wt. Ru/ 15% wt. Ni/ Al2O3 | 400oC | 88 | 82 | (Al and Al, 2020) [7]
Table1: Supported Ru-based catalyst for CO2 methanation. H2/CO2 ratio of 4 ; X CO2 = conversion of CO2 ; S CH4 = selectivity to CH4. All the samples were prepared by impregnation of the metal over the support
Notes: In a valuable study, Xu et al. (2016) examined the influence of TiO₂ as a support material. The Ru/TiO₂ catalyst demonstrated over three times the methanation rate of Ru/Al₂O₃. This improvement was linked to the smaller average Ru particle size (2.8 nm compared to 4.3 nm), which was promoted by the rutile form of TiO₂. The presence of this stable crystalline phase effectively limits particle agglomeration and enhances metal dispersion, contributing to the increased activity.

## Slide 6
METHODOLOGY
Catalyst Preparation
Precursor
Pretreated Support
Heated in an oil bath at 323K to evaporate all the solvent
Placed in an oven and dried at 378K over night
Calcination at 473K(4h) and cooled to room temperature
Washed with dilute ammonia and water(3times each)
Catalyst | Ru Loading | Key properties
1 wt% Ru/TiO2 | Moderate | Balanced activity and dispersion; Common in methanation
3 wt% Ru/TiO2 | High | Higher activity, but risk of sintering
5 wt% Ru/TiO2 | Very High | Higher CO conversion, but possible drop in selectivity
Fig 4: Schematic for catalysts synthesis using incipient wetness impregnation method
RuCl₃·xH₂O solution
Pressed into pellets, crushed and sieved(150-200µm)

## Slide 7
METHODOLOGY CONT.
CO2
H2
He
MFC
Temperature Controller
Spectrometer
Display Output
Loading the catalyst onto the reaction chamber
Placing the reaction chamber onto the praying mantis apparatus
Pipelines
Valves
EXPERIMENTAL SET-UP
Flow in
Flow Out
Chiller in
Chiller out
Thermocouple attached to TC
Fig 5: Schematic of the Experimental Set-up

## Slide 8
METHODOLOGY CONT.
Catalyst Preparation
EXPERIMENTAL PROCEDURE for Ru/TiO2
Catalyst Reduction
He Purge
Background Spectrum Collection
Load 1 wt% Ru/TiO₂ catalyst into the DRIFTS (Praying Mantis) reaction cell.
Reduce at 250 °C for 3.5 hours under H₂. MFCs calibrated for H₂ and He.
Purge system with He for 30 minutes to remove residual gases.
Cool to 50 °C, introduce liquid nitrogen, and collect background spectra.
CO2 Adsorption
Post-Adsorption Purge
Methanation Preparation
CO2 Methanation
Introduce CO2 at 150-400°C (50 °C intervals) and also collected spectra at 200oC for 1 hour
Purge with He for 30 minutes to clear surface.
Re-calibrate MFCs for CO₂ and H₂ flow.
Introduce CO2 + H2 at 150-400 °C. Time-dependent methanation study at 300 °C for 1 hour

## Slide 9
RESULTS & DISCUSSION – CO2 ADSORPTION
Key Observations
Maximum absorption observed at 200oC
Formation of bicarbonate (HCO3-) species observed at 1612 cm-1. Hydroxyl band gradually decreases
HCO3- bands disappear. Simultaneous emergence of HCOO- species
Fig 8: in-situ DRIFT spectra during CO2 adsorption over 1 % Ru/TiO2
Fig 9: in-situ DRIFT spectra during CO2 adsorption at 200oC for 1 hour

## Slide 10
RESULTS & DISCUSSION - CO2 METHANATION
Key Observations
The bands of CH4 at 1304 and 3017 cm-1 are present with the bands of CH3*(2960) and HCOO*(1369 and 1573 cm-1)
HCO₃⁻ bands(1623 cm-1) disappear at 200 °C, replaced by HCOO⁻ (1369, 1573 cm⁻¹) → maximum at 300 °C.
CO spikes suddenly when HCO₃⁻ vanishes indicating a secondary CO route
Fig 6: in-situ DRIFT spectra during CO2 methanation over 1 % Ru/TiO2
Fig 7: in-situ DRIFT spectra during CO2 methanation at 300C for 1 hour

## Slide 11
TiO2
TiO2
TiO2
TiO2
TiO2
TiO2
H* + H*
CO2(g)
CO2*
HCO3*
HCOO*
CH*
CH3*
CH4(g)
H*
H*
H*
H*
FORMATE PATHWAY
H*
Fig 10: Proposed formate pathway for CO2 methanation over 1% Ru/TiO2 catalysts
Followed at lower temperatures
H*

## Slide 12
RWGS + CO Methanation pathway
TiO2
TiO2
TiO2
TiO2
TiO2
TiO2
H* + H*
CO2(g)
CO2*
HCO3*
CO*
CH3*
CH4(g)
HCOO*
H*
H*
H*
H*
H*
Fig 11: Proposed RGWS + Methanation pathway for CO2 methanation over 1% Ru/TiO2 catalysts
Followed at Higher temperatures

## Slide 13
Comparison with Other Supports
Fig 12: Ru/TiO2
Fig 13: Ru/ZrO2 (M. Liu et al.) [8]
Ru/Al2O3(P. Dongapure. et al.) [9]
HCO32- forms at ~ 150oC
HCOO- dominates 200-300oC
Weak CO bands emerge only at > 300oC
Intense HCO3- formation
Strong HCOO- Peaks at 200 o C
Presence of Bridged CO bands confirm CO intermediates
Carbonate peaks (1435 & 1652 cm-1 ) seen at 175oC.
Strong CO bands (1850-2100cm-1).
Back donation of the metal to CO antibonding orbitals on adsorption.
Weaker formate activity, CO pathway at higher temperature
Fastest, most efficient formate route (OH- rich)
Dominant CO pathway

## Slide 14
Temperature Dependency
Lower Temperature: Formate Pathway observed (150oC-250oC), Formation of bicarbonates and formates
Higher Temperature: Appearance of CH4 bands (from 350oC onwards) and decline in CO-related bands
Time Dependency
At fixed temperatures (300 °C for methanation, 200 °C for adsorption), spectra remained time-invariant.
Support Comparison
Ru/ZrO2 : Strong formate-route preference
Ru/Al2O3: Favors CO hydrogenation
Ru/TiO2 : Dual Pathway (Formate at lower temperature + CO at higher temperature)
CONCLUSION

## Slide 15
Future Prospect
WP-1 Synthesis of catalysts, followed by drifts characterisation
WP-2 Effect of Temperature, Pressure, Flow rate and Promoters on TOF/Rate/Conversions by activity tests along with in-situ FTIR
WP-3 Kinetic modelling followed by validation of experimental activity study (from WP-2)
Activity along with mechanistic pathways findings
Global rate model
Intrinsic (ki)
Apparent (ka)
Extrinsic (ke)
kg = f(ki , ka , ke)
Kg = f(T, P, NRe, NPr, NSc, NSh, catalyst, reactor geometry)
WP-4 CFD reaction model development of the developed model using Ansys Chemikin-Pro / COMSOL Multiphysics
IWI
EDX, TEM, Chemisorption

## Slide 16
REFERENCES
Research Progress and Reaction Mechanism of CO2 Methanation over Ni-Based Catalysts at Low Temperature: A Review, Li LI et al.
Strong metal–support interaction of Ru on TiO2 derived from the co-reduction mechanism, Y. Zhang et al.
Diffuse Infrared Fourier Transform Spectroscopy in Environmental Chemistry, Azambre, et al.
Hydrogenation of CO2 over supported noble metal catalysts, Panagiotopoulou et al.
Methanation of carbon dioxide on Ru/Al2O3 and Ni/Al2O3 catalysts at atmospheric pressure: Catalysts activation, behaviour and stability, Garbarino et al.
Effect of metal loading on the CO2 methanation: A comparison between alumina supported Ni and Ru catalysts, Quindimil et al.
Improving CO2 methanation performance by distributed feeding in a Ni-Mn catalyst fixed bed reactor, Aldea et al.
Improvement in the activity of Ru/ZrO2 for CO2 methanation by the enhanced hydrophilicity of zirconia, Liu et al.
Variations in activity of Ru/TiO 2 and Ru/Al2O3 catalysts for CO2 hydrogenation: An investigation by in-situ infrared spectroscopy studies, P. Dungapure et al.

## Slide 17
Q&A